## Slide 1
is so nice. The crop locations from the Gwyddion are below:
30 mA before: Origin X 48 px, Origin Y 131 px.
30 mA after: Origin X 16 px, Origin Y 149 px.
n30 mA before: Origin X 47 px, Origin Y 103 px.
n30 mA after: Origin X 37 px, Origin Y 99 px.
Also, the crop size is always 3.42 microns width and 2.2 heigh microns.
Done 30mA before done Image

## Slide 2
MFM image when the track is fully saturated in +700 Oe. The dark regions in the dashed yellow circles are defects on the track surface
(c) and (d) are the MFM images in +30 Oe before and after a +30 mA current was applied to the heater, respectively. Dashed red lines indicate position of the leading edge of the reverse domains.
(e) and (f) MFM images in +30 Oe before and after a -30 mA current was applied to the heater, respectively. Dashed blue and black lines indicate the positions of the line profiles that are shown in
Location of SKYRMIONS

## Slide 4
(c) MFM images in +30 Oe before a +30 mA current was applied to the heater, respectively. Dashed red lines indicate position of the leading edge of the reverse domains.
c)
30 mA before: Origin X 48 px, Origin Y 131 px.

## Slide 5
d)
before
after

## Slide 6
e)

## Slide 7
f)
30 Oe after

## Slide 8
f)
-30 Oe after

## Slide 9
f)
-30 Oe after

## Slide 10
f)
-30 Oe after

## Slide 11
Just to see what it looks like at 15um scan
5 m

## Slide 12
Just to see what it looks like at 15um scan

## Slide 13
15um scans
-70 Oe
-110 Oe
-125 Oe
-135 Oe
-150 Oe
-157 Oe

## Slide 14
30mAbefore
n30mAafter
n30mAbeforer
30mAafter