ABOUT THE DATASET

Title: Optically selective photomask based on field-induced periodic defect arrays in ferroelectric nematics

Creator(s): Rajalaxmi Sahoo[1], Mamatha Nagaraj[1], Thomas Raistrick[1], Gordon D. Love[2], Helen F. Gleeson[1]

Organisation(s):

[1]. School of Physics and Astronomy, University of Leeds, Leeds, LS2 9JT, UK.

[2]. School of Computer Science, University of Leeds, Leeds, LS2 9JT, UK.

Rights-holder(s):Unless otherwise stated, Copyright 2025 University of Leeds

Description: We demonstrate the formation of field-induced periodic defect arrays in the ferroelectric nematic liquid crystal (FNLC) phase upon the application of electric field. The measurements are performed in two different room-temperature FNLC materials, which are filled in LC devices having bare electrodes. The periodicity of the defect patterns are tunable by varying the field parameters as well as cell gap. We then use the field-induced periodic patterns as a photomask for light modulation to create periodic phase arrays.

Cite as: Please use the default citation format

Rajalaxmi Sahoo, Mamatha Nagaraj, Thomas Raistrick, Gordon D. Love, Helen F. Gleeson (2025) Dataset for 'Optically selective photomask based on field-induced periodic defect arrays in ferroelectric nematics'.University of Leeds. https://doi.org/10.5518/1777.

Related publication: R.Sahoo, M.Nagaraj, T.Raistrick, G. D.Love, and H. F.Gleeson, “Optically Selective Photomask Based on Field-Induced Periodic Defect Arrays in Ferroelectric Nematics.” Advanced Optical Materials (2026): e03769. https://doi.org/10.1002/adom.202503769

Contact: r.sahoo@leeds.ac.uk

PROJECT AND FUNDING INFORMATION

Date: 15th August 2022- 14th August 2027

Funding organisation: Engineering and Physical Sciences Research Council and Merck Performance Materials Ltd.

Grant no.: EP/V054724/1

CONTENTS

Files include

- All the POM images shown in the main manuscript and the supplementary information

- The data shown in Figure 2(b), FigureS2 (a,b) and FigureS3 (c)

- Figure1.jpg: Polarized optical microscope (POM) images of the two-dimensional periodic defect patterns induced in the NF phase upon the application of an electric field. The measurement is done at T= 24 deg c, and by varying the field parameters.

- Figure2a.jpg: POM images of the periodic defect patterns obtained at 6 V, while varying the applied frequency.

- Figure2b.xlsx: Applied frequency (x-axis) vs periodicity (y-axis) at fixed voltage of 6 V. Inset of the figure shows the applied voltage (x-axis) vs periodicity (y-axis) at 5 kHz.

- Figure3.jpg: POM images of the periodic defect patterns without and with the retardation plate. Additional domain features observed under varied voltages while the frequency is fixed at 3 kHz.

- Figure5.jpg: POM images of periodic phase arrays formed after exposure through the NF photomask.

- Figure6.jpg. Images of the transmitted light captured using a beam profiler.

- FigureS1.jpg: NF phase texture

- FigureS2_c-e: POM images of periodic defect patterns obtained for different cell gaps, d=4 µm, 7 µm and 10 µm.

- FigureS2a,b.xlsx: Amplitude of the applied voltage (x-axis) vs periodicity (y-axis) for different cell gaps, d=4 µm, 7 µm and 10 µm.

- FigureS3_a,b: POM images of periodic defect patterns in the NF phase of (a) FNLC-919 and (b) M5.

- FigureS3c.xlsx: Amplitude of the applied voltage (x-axis) vs periodicity (y-axis) for both materials (FNLC-919 and M5).

METHODS

Details of all of the methods used to collect this data can be found in the associated publication, “Optically Selective Photomask Based on Field-Induced Periodic Defect Arrays in Ferroelectric Nematics.” Published in Advanced Optical Materials (2026): e03769.