## Slide 1: Syringe Samples

## Slide 2
1 2 3 4 5
5 macropores
0 mmHg - Syringe

## Slide 3
1 2 3 4 5
6 or 7 macropores, (is there one in the 5th sample)
250 mmHg - Syringe

## Slide 4
1 2 3 4 5
2 macropores
550 mmHg - Syringe

## Slide 5
1 2 3 4 5
3 macropores
0 mmHg - Syringe

## Slide 6: Vac Bowl Samples

## Slide 7
1 2 3 4 5
0 macropores
0 mmHg – Vac Bowl

## Slide 8
1 2 3 4 5
3 macropores
250 mmHg – Vac Bowl

## Slide 9
1 2 3 4 5
550 mmHg – Vac Bowl
1 macropores (Anomaly)

## Slide 10
1 2 3 4 5
650 mmHg – Vac Bowl
0 macropores

## Slide 11: Open Bowl Samples

## Slide 12
1 2 3 4 5
6 macropores
0 mmHg – Open Bowl